TECHNICAL INFORMATION ABOUT UHG PANEL 122

| No | PROPERTY | TEST METHOD | UNITS | VALUE |
| --- | --- | --- | --- | --- |
| 1 | Surface Abrasion Resistance | EN 14323 cls. 5.9 | Revolutions (class 2) | 300 |
| 2 | Scratch Resistance | DIN 68861 part 4 | N (class 4E) | 1,0 |
| 3 | Determination of Bulk Density of Wood Basis Chipboard | EN 323 | Kg/m³ | 784,8 |
| 4 | Behavior Towards Impact Loading by Falling Steel Ball | EN 14323 cls. 5.14 | Occurred Dent | No Cracking |
| 5 | Resistance to Staining | EN 14323 cls. 5.6 | No Change | No Change |
| 6 | Gloss Level (60° angle) | EN 14323 part 5.13 | Gloss units | ˃95 |
| 7 | Test of Water Steam Resistance | EN 14323 cls. 5.11 | No Change | No Change |
| 8 | Bending Strength (*) | EN 310 | N/mm² | 46,2 |
| 9 | Modulus of elasticity in bending (*) | EN 310 | N/mm² | 4145 |
| 10 | Surface Soundness (Tensile Strength) (*) | EN 311 | N/mm² | 1,5 |
| 11 | Tensile Strength vertical to the surface (*) | EN 319 | N/mm² | 0,49 |
| 12 | Assessment of surface resistance to wet heat | EN 12721:2009 | No Change | No Change to 85°C |
| 13 | Assessment of surface resistance to dry heat | EN 12722:2009 | No Change | No Change to 70°C |
| 14 | Colorfastness to light | EN 15187 | Grade | 6+ |
| 15 | Assessment of surface resistance to cold liquids (contact time 16 hours). | EN 12720 | No Change | No Change |

(*)These values are weighted average of the test results

Annex 1 is the result reports of 6, 7, 10, 12 and 13 th tests.

Annex 2 is the result reports of 1, 2, 3, 4, 5, 8, 9 and 11 th tests.

Annex 3 is the result reports of 14 th test.

Annex 4 is the result report of 15 th test.